PU H 1.5 SUCTION HOSE

Properties:

• highly abrasion-proof

• smooth interior

• increased pressure and vacuum

resistance

• high tensile strength and tear resistant

• good resistance to chemicals

• small bending radius

• gas and liquid tight

• capable of electrostatic discharge by

grounding the spiral

• electrical and surface resistance ≤1010 Ω
Temperature Range:

• -40°C approx. to +90°C approx.

• short time to +125°C approx.

Specification:

• ø 32 to ø 203 mm
• Overpressure 3,095 to 0.6 bar
• Vacuum 0.875 to 0.120 bar
Applications:

• for high flow-rates of hot and abrasive

solids such as powder, chip and granules

• for industrial vacuum cleaners, granule

conveying systems, printing machines,

blowers and compressors

• as robust protection hose

Construction:

• spring steel wire integrated in wall

• wall thickness 1.5mm approx.

Material:

• wall: special premium ester-polyurethane

• spiral: spring steel wire

Stardard color:

• transparent

[image: image1.jpg]



Шланг всасывающий PU H 1.5

Свойства:

• Высокая абразивостойкость

• Гладкая внутренняя поверхность

• повышенный вакуум и давление
• высокая прочность на разрыв
• хорошая стойкость к химикатам

• маленький радиус изгиба

• газонепроницаемый и герметичный
• способный отводить электростатические заряды через 

заземление спирали
• электрическое поверхностное сопротивление ≤1010 Ω

Температура эксплуатации:

• -40°C до +90°C ориентировочно
• кратковременно до +125°C ориентировочно
Спецификация:

• ø 32 to ø 203 mm
• Избыточное давление 3,095 до 0,6 бар

• Вакуум 0,875 до 0,12 бар
Применение:

• для высоких скоростей потока горячих и абразивных материалов

твердых веществ, такие как порошок, крошка и гранулы

• для промышленных пылесосов, конвейерных систем для гранул, печатных машин, воздуходувок и компрессоров

• в качестве прочного защитного шланга

Конструкция:

• проволока из пружинистой стали встроенная в стенку из полиуретана
• толщина стенки до 1.5mm ориентировочно
Материал:

• стенка:специальный премиум Этер-полиуретан
• спираль: проволока из пружинистой стали
Стандарный цвет:

• Прозрачный
