PU L 1.0 SUCTION HOSE

Properties:

• highly abrasion-proof

• smooth interior

• high tensile strength and tear resistant

• microbe and hydrolysis resistant

• good resistance to chemicals

• good resistance to UV and ozone

• small bending radius

• gas and liquid tight

• capable of electrostatic discharge by

grounding the spiral

• electrical and surface resistance ≤1010 Ω
Temperature Range:

• -40°C approx. to +90°C approx.

• short time to +125°C approx.

Specification:

• ø 32 to ø 254 mm
• Overpressure 2,12 to 0.28 bar

• Vacuum 0.46 to 0.02 bar
Applications:

• for abrasive solids such as dust, powder,

fibre, chip, and granules

• for de-dusting and suction plant, industrial

vacuum cleaners, suction of paper and

textile fibre

Construction:

• spring steel wire integrated in wall

• wall thickness 0.9mm approx.

Material:

• wall: special premium ether-polyurethane

• spiral: spring steel wire

Standard Color:

• transparent

[image: image1.jpg]




Шланг всасывающий PU L 1.0
Свойства:

• Высокая абразивостойкость

• Гладкая внутренняя поверхность 

• высокая прочность на разрыв
• стойкость к микробам и гидролизу
• хорошая стойкость к химикатам
• хорошая стойкость к ультрафиолету и озону
• маленький радиус изгиба
• газонепроницаемый и герметичный
• способный отводить электростатические заряды через 

заземление спирали

• электрическое поверхностное сопротивление ≤1010 Ω

Температура эксплуатации:

• -40°C до +90°C ориентировочно
• кратковременно до +125°C ориентировочно
Спецификация:

• ø 32 to ø 254 mm
• Избыточное давление 2,12 до 0,28 бар

• Вакуум 0,46 до 0,20 бар

Применение:

• для абразивных твердых веществ, таких как пыль, порошок,

волокно, щепа и гранулы

• для пылеулавливающей и аспирационной установки, промышленных пылесосов, всасывание бумаги и

текстильных волокон

Конструкция:

• проволока из пружинистой стали встроенная в стенку из полиуретана
• толщина стенки 0.9mm ориентировочно
Материал:

• стенка: специальный премиум Этер-полиуретан
• спираль: проволока из пружинистой стали
Стандарный цвет:

• Прозрачный
